## Slide 1: Development of New Lunar Soil Simulants in Japan
Space Resource Roundtable - VIII
Oct. 31- Nov. 2, 2006
Hiroshi TAKEDA
Chiba Institute of Technology
Kai MATSUI
Akira MIYAHARA
Lunar Exploration Technology Office
JAXA
Hiroshi KANAMORI
Shigeru AOKI
Institute of Technology
SHIMIZU Corporation

## Slide 2: Background
1. Activated Research on Lunar Exploration (Large Demands for the Simulants)
2. Running out of MLS-1, JSC-1, and FJS-1
(Small Supply of the Simulants)
Development of
‘New’ Lunar Soil Simulant
> International collaboration
> Standardization

## Slide 3: Goals
To develop various types of Lunar Soil Simulant, which meet …
the regional needs,
(mare, highland, etc.)
the property needs, and
(mechanical, chemical, etc.)
the supply needs.
(quickly, enough amount, reasonable price)

## Slide 4: Study Flow
1. Sampling of
Raw Materials
a. Selection of Mining Site
b. In-situ Investigation
c. Acquisition of the Samples
a. Chemical Composition (Bulk)
b. Modal Abundance (EPMA)
c. Particle Density
2. Characterization
3. Determination of Mix Proportions /Evaluation
4. Trial Manufacturing of New Simulants

## Slide 5: Criteria for the Selection of Raw Materials
1. Approximated to the Bulk Chemical Composition of Lunar Mare/ Highland Samples
> Used as Base (Root)
2. Pure Minerals Contained in Lunar Samples
> Used as Additives
3. Adaptable to the Mass-Production

## Slide 6: Possible Raw Materials (1)
Base
1.* Bytownite (Minnesota)
2. Albite (Norway)
3. Labradorite (Madagascar)
12. Anorthosite (Stillwater)
13. Basalt (Hawaii)
15. Basalt (Oshima, Japan)
19. FJS-1 (Basalt/ Mt. Fuji, Japan)
21. Gabbro (Kohyama, Japan)
22. Bytownite (Mexico)
* Sampling Number

## Slide 7: Possible Raw Materials (2)
Additives
4.* Forsterite (Arizona)
6. Forsterite (S. California)
7. Forsterite (Hokkaido, Japan)
8. Forsterite (Pakistan)
9. Bronzite (California)
10. Enstatite (Norway)
11. Ilmenite (Australia)
* Sampling Number

## Slide 8: Evaluation of Raw Materials (Comparison with Apollo Samples)
Method
Σ (Li – Ci)2
R =
i = 1
7
7
Selected a Condition that makes Minimum R Value.
SiO2
TiO2
Al2O3
MgO
CaO
Na2O
K2O
Focused on 7 Components
Li: Content of #i Component in the Apollo Sample
Ci: Content of #i Component in a Raw/ Mixed
Material

## Slide 9: Chemical Composition of Typical Apollo Samples
Components
A-11
A-12
A-14
A-15
A-16
A-17
SiO2
TiO2
Al2O3
MgO
CaO
Na2O
K2O
42.2
7.8
13.6
7.8
11.9
0.47
0.16
46.3
3.0
12.9
9.3
10.7
0.54
0.31
48.4
1.7
17.4
9.4
10.7
0.7
0.55
46.9
1.4
14.6
11.5
10.8
0.39
0.21
45.0
0.54
27.3
5.7
15.7
0.46
0.17
43.2
4.2
17.1
10.4
11.8
0.40
0.13
(wt%)

## Slide 10: Recommended Raw Materials – the Chemical Composition (Bulk)
Single Case
A-11
A-12
A-14
A-15
A-16
A-17
13-A: Basalt (Hawaii)
21: Gabbro (Kohyama, Japan)
13-A: Basalt (Hawaii)
12-A: Anorthosite (Stillwater)
12-A: Anorthosite (Stillwater)
21: Gabbro (Kohyama, Japan)
12-A: Anorthosite (Stillwater)
13-A: Basalt (Hawaii)
1: Bytownite (Minnesota)
21: Gabbro (Kohyama, Japan)
21: Gabbro (Kohyama, Japan)
12-A: Anorthosite (Stillwater)
4.705
5.208
2.826
3.521
1.951
2.367
2.907
3.119
3.941
3.956
3.400
3.996
R

## Slide 11: Recommended Raw Materials – the Chemical Composition (Bulk)
Mixed Case
A-11
A-12
A-14
A-15
A-16
A-17
1: Bytownite (Minnesota)
1.336
1.591
0.737
1.220
2.728
1.616
R
6: Forsterite (S. California)
8-A: Forsterite (Pakistan)
11: Ilmenite (Australia)
12-A: Anorthosite (Stillwater)
21: Gabbro (Kohyama, Japan)
87
1
9
8
4
18
10
5
6
5
12
81
81
76
85
84
19
（Mix Proportion: wt%）
9: Bronzite (California)
9

## Slide 12: Recommended Mixture of Raw Materials – Modal Abundances
Mare
Highland
11: Ilmenite (Australia)
12-A: Anorthosite (Stillwater) / Plagioclase
15-C: Basalt (Oshima, Japan) / Glass
21: Gabbro (Kohyama, Japan) / Olivine
21: Gabbro (Kohyama, Japan) / Opx
21: Gabbro (Kohyama, Japan) / Augite
8.5
0.5
15.5
42.0
56.5
51.5
2.5
2.0
6.5
3.0
10.5
1.0
(Mix Proportion: wt%)
100
100
Total

## Slide 13: Modal Abundance of Minerals in Typical Apollo Samples
Minerals
Plagioclase
Ilmenite
Olivine
Glass
Pyroxene
Volcanic
Agglutinitic
Opx
Pigeon
Mg- Cpx
Fe- Cpx
16.80
6.40
1.40
3.40
53.90
0.34
3.94
10.35
1.38
(wt%)
10084
71061
61141
Apollo Samples
13.90
10.40
3.90
18.90
31.40
1.15
6.87
10.29
2.18
42.50
0.30
2.10
0.00
50.10
1.68
1.38
1.11
0.18

## Slide 14: Chemical Composition of New Lunar Soil Simulants
(wt%)
Element
SiO2
TiO2
Al2O3
Cr2O3
FeO
Fe2O3
MnO
MgO
CaO
Na2O
K2O
P2O5
S
H2O
Total
A-11
42.20
7.80
13.60
0.30
15.30
0.00
0.20
7.80
11.90
0.47
0.16
0.05
0.12
0.00
99.90
A-12
46.30
3.00
12.90
0.34
15.10
0.00
0.22
9.30
10.70
0.54
0.31
0.40
-
0.00
99.11
A-14
48.10
1.70
17.40
0.23
10.40
0.00
0.14
9.40
10.70
0.70
0.55
0.51
-
0.00
99.83
A-15
46.80
1.40
14.60
0.36
14.30
0.00
0.19
11.50
10.80
0.39
0.21
0.18
0.06
0.00
100.79
A-16
45.00
0.54
27.30
0.33
5.10
0.00
0.30
5.70
15.70
0.46
0.17
0.11
0.07
0.00
100.78
A-17
43.20
4.20
17.10
0.33
12.20
0.00
0.17
10.40
11.80
0.40
0.13
0.12
0.09
0.00
100.14
FJS-1
49.14
1.91
16.23
0.00
8.30
4.77
0.19
3.84
9.13
2.75
1.01
0.44
0.00
0.43
98.14
Oshima
Base
49.13
5.47
12.33
0.04
6.02
9.90
0.36
6.15
6.67
2.16
0.32
0.12
0.01
0.38
99.06
Kohyama
Base
47.49
0.14
22.59
0.02
7.80
0.73
0.17
10.24
8.02
1.65
0.07
0.06
0.01
0.03
99.02

## Slide 15: Future Works
Simulating Methods
> Additional Investigation on the Raw Materials
> Agglutinate and Glass
> Grain Level Properties
> Mass-productivity
> Simulated Lunar Ground
- Reproduction of Bulk Density Distribution
- Mixing Condition of stones/ ice (> 2mm)

## Slide 16
End